CABLE SPECIFICATION

Issued: August 12, 2010

Revised: ---

ITEM:    10-002-12D-AANONF

Fiber Diameter (core/clad)	microns                        50/125*

Fiber Type	Multimode                   Graded Index

Numerical Aperture	--                                  0.20, ±0.015

Maximum Attenuation @ 850/1300nm	dB/km                          3.0/1.0

Bandwidth @ 850/1300 nm

(Overfilled lauch, LED based sources)	Mhz.km                       750/500

Transmission Link Lengths at 850nm

& 1300nm(LX4) for 10Gb/s*	meters			150/150

Number of Fibers	--                                   2

Buffer Diameter	microns                         900

Storage Temperature Range	°C                                 -40 to +70

Operating Temperature Range	°C                                 -20 to +70

Max. Tensile Load for Installation	N (lbf)                          1000 (225)

Max. Tensile Load, Long-Term	N (lbf)                           500 (112)

Min. Bend Radius, Unloaded	--                                   10 X O.D.

Crush Resistance (EIA 455-41)	N/cm                             100

Impact Resistance (EIA 455-25)	Impacts                         25

Flexing, 90° (EIA 455-104)	Cycles                           25

Cable Outside Diameter, Nom.	mm (in.)                        2.9 X 6.0(0.114 x 0.235)

Cable Weight, Nom.	kg/km (lbs./1000)          18 (12)

DESCRIPTION:  2 tight-buffered fibers, aramid yarns, Aqua riser rated PVC outer jacket in a zip cord construction, OFNR C(ETL)US.

**Note: The values listed herein are nominal.  Remee Products Corporation reserves the right to modify.