1.0	SCOPE

This document establishes the specification requirements for a multimode OM3 distribution indoor/outdoor fiberoptic cable.  This cable construction consists of multimode fibers in a distribution tight-buffered design with a riser rated PVC jacket suitable for outdoors in duct, indoors in the riser and acceptable in tray installation as well.

2.0	APPLICABLE DOCUMENTS

Reference Documents:	TIA/EIA FOTP Standards 455

Color Coding of Fiber Optic Cables TIA/EIA-598

UL 1666

GR-409-CORE

3.0	REQUIREMENTS

This document contains test values for all-important mechanical, optical, and environmental parameters and as such, is the basis for all-incoming inspection and acceptance.

- CABLE CROSS SECTION

| Cross Section | Components |
| --- | --- |
|  | Tight Buffered Fibers Water Swellable Kevlar Yarns Outer Jacket |

- OVERALL CABLE CONSTRUCTION

5.1	Tight Buffered Fiber

Dimension: 900µm, nominal.

Tight buffered fiber color code: 1-blue, 2-orange, 3-green, 4-brown, 5-slate, 6-white, 7-red, 8-black, 9-yellow, 10-violet, 11-rose, and 12-aqua.

5.2	Cable strength

Aramid yarns with water swellable characteristics are pulled in with the tight-buffered fibers under the outer jacket.

5.3	Outer Sheath

Pressure extruded UV resistant Aqua riser rated PVC jacket (or color per customer request)

5.4	Cable Markings

REMFO 11 SERIES, FIBER OPTIC CABLE, XX (No. of fibers)-50/125, 10GIG OM3, REMEE PRODUCTS CORP., MM/YY (month & year of manufacture), OFNR C(ETL)US, Sequentially meter marked.

Special print as required by customer.

5.5  Nominal Cable Dimensions & Weights

| Remee Products Part Number | No. of Fibers | Cable OD (mm) | Cable OD (in.) | Weight KG/KM | Weight LB/1000ft |
| --- | --- | --- | --- | --- | --- |
| 11-002-12S-AANOOF | 2 | 4.6 | .180 | 19 | 13 |
| 11-004-12S-AANOOF | 4 | 5.0 | .195 | 22 | 15 |
| 11-006-12S-AANOOF | 6 | 5.3 | .210 | 27 | 18 |
| 11-008-12S-AANOOF | 8 | 5.7 | .225 | 31 | 21 |
| 11-012-12S-AANOOF | 12 | 6.6 | .260 | 40 | 27 |

- FIBER CHARACTERISTICS

6.1	Physical Parameters (nominal)

| Fiber Type | Multimode* |
| --- | --- |
| Maximum Attenuation @ 850/1300nm** | 3.0 /1.0 dB/km |
| LED Performance (Overfilled Launch Bandwidth) | 1500/500MHz-km@850/1300 |
| Laser EMB Performance | 2000/500MHz-km@850/1300 |
| Core Diameter, nominal | 50 ± 3.0 µm |
| Cladding Diameter | 125.0 ± 2.0 µm |
| Primary Coating Diameter | 245 ± 5 µm |
| Cladding Non-circularity | <2% |
| Core-Clad Concentricity | 3.0 µm |
| Zero Dispersion Wavelength | 1300-1320nm |
| Maximum Zero Dispersion Slope | 0.101 ps/nm2-km |
| Numerical Aperture | 0.20 ± .015 |
| Group Refractive Index @ 850/1300nm | 1.481/1.476 |
| Proof Test | 100 kpsi |

*Guaranteed Gigabit Ethernet Distance of 300mtr at 850nm for 10 Gb/s per IEEE802.3ae and 1000mtr at 850nm for 1 Gb/s per IEEE802.3z.

**Measured attenuations on shipping reels will not exceed the nominal values by .75dB/km.

7.0	MECHANICAL & ENVIRONMENTAL PERFORMANCE

Maximum Tensile Load for:

Installation:  2&4-fiber 1405N/315lbf, 6&8-fiber 1610N/362lbf	Impact Resistance: 25 Impacts (min.)

12-fiber  2700N/600lbf				Flexing, ±90°: 25 Cycles (min.)

Long Term:  2&4-fiber 455N/102lbf, 6&8-fiber 535N/120lbf	Temperature rating:

12-fiber 600N/135lbf					Operation,	-40°C to +85°C

Minimum bending radius:							Installation,	   0°C to +75°C

Loaded: 20 x diameter						Storage,	-55°C to +85°C

Unloaded: 10 x diameter				Crush Resistance: 100N/cm

- PREPARATION FOR DELIVERY

The cable shall be packaged to preclude the inducement of damage due to handling and transportation, and shall be in accordance with the best commercial practices available.